## Slide 1: Moon to Mars Oxygen and Steel Technology (MMOST) Update
Presented at:
XXII Space Resources Roundtable
June 9, 2022
Mark Berggren, Robert Zubrin, Michael Riley, and Stacy Carrera
Pioneer Astronautics
Lakewood, ColoradoCarrerra

## Slide 2: Moon to Mars Oxygen and Steel Technology (MMOST)
Pioneer Astronautics
Colorado School of Mines
Honeybee Robotics
NASA JSC SBIR Phase II Sequential Contract 80NSSC20C0250
September 15, 2020 – September 14, 2022

## Slide 3
Moon to Mars Oxygen and Steel Technology
Beneficiation
Reduction
Melt Refining
Additive Manufacturing
Lunar
Regolith
Reject
FeO
FeTiO3
Mixed
Oxides
O2
Mixed Oxides
Steel Parts
Fe
Mixed
Oxides
Fe
Two-year design/build/test/demonstration program
Final design targets 35 kg/day Fe and 10 kg/day O2 with integrated operation
  Demonstration at 1/10th scale
Lunar Oxygen ISRU Experiment (LOXIE) demonstration added
Pioneer Astronautics
Colorado
School of
Mines
Honeybee Robotics
Vacuum Testing
Simulants

## Slide 4
Lunar Materials Handling System
(Repetitive Feeding/Discharging;
Process Automation; Hydrogen Reduction)
Lunar Soil Particle Separator
(Beneficiation)
Pioneer Precursor Technologies – NASA SBIR Phase I/II
Moon to Mars Oxygen and Steel Technology

## Slide 5
Extraterrestrial Metals Processing
(H2/CO Reduction; Melt Refining)
Precursor Technologies – NASA SBIR Phase I/II (continued)
Iron Oxide
Reduction Reactor
Iron Product
Iron Product
and Machining
Moon to Mars Oxygen and Steel Technology
Reduced Regolith
Melting Furnace

## Slide 6
Colorado School of Mines – Supporting Technologies
Tubular Mill and Wire Drawing
(Preparation for Additive Manufacturing)
Additive Manufacturing Evaluation
High-Vacuum Chambers
Moon to Mars Oxygen and Steel Technology
Honeybee Robotics – 3.5 Meter Lunar Vacuum Chamber

## Slide 7
MMOST Block Flow Diagram
MMOST Metal Production Steps

## Slide 8
Flow Sheet Development
Process Development and Scale-Up:
Initial system for 3.5 kg/day iron (1 kg/day oxygen)
  LOXIE demonstration of 0.5 kg/day of oxygen
  Scaled-up system design for 35 kg/day iron (10 kg/day oxygen)
Advance TRL from 4 to 6
Parallel Support Activities:
Lab-scale experiments
Simulant formulation
Data acquisition and control
Automation
Testing of modules in vacuum
Moon to Mars Oxygen and Steel Technology

## Slide 9
Simulant selection:
Match lunar physical and chemical properties to the extent possible using terrestrial minerals
Baseline (Ilmenite case)
  basalt (JSC-1A equivalent)
  Ilmenite
  agglutinate simulant
Baseline (FeO case)
  basalts of varying FeO concentration
  agglutinate simulant
Identify higher-fidelity simulant formulations as the program progresses
Moon to Mars Oxygen and Steel Technology

## Slide 10
Current Results
10wt% Ilmenite feed upgraded to 25wt%
Unit recently tested in Pioneer vacuum chamber
Magnetic Drum and Slotted-Ramp Particle Size Separator in Pioneer Vacuum Chamber
Beneficitiation: Magnetic and Slotted Ramp

## Slide 11
Details and Current Results:
Design basics
  >10 kV; low current
  Horizontal tribocharging feed
Latest estimated results
  Upgrading of 25wt% Ilmenite feed to about 40 to 50wt% based on initial results
  Further analysis and more accurate results pending
Electrostatic Separator
Material Dispersed by the Electrostatic Separator
Beneficiation: Electrostatic
Vibrational Feeder with Heating Lamps and Tribocharging Plate
Power Supply and Controls

## Slide 12
Select results
Beneficiation has significant impact on reduction
  Power consumption
  Percent conversion
Operation with electrolyzer system demonstrated
Temporarily integrated electrolysis unit
Semi-automatic lab reduction unit
Reduction: Lab Scale Experiments

## Slide 13
Operational demonstration modes
MMOST
  Designed for 3.5 kg/day Fe/1.0 kg/day O2 output
  Operates on hydrogen tank feed at this demonstration level
LOXIE
  Uses MMOST technology, but O2 output target 0.5kg/day
  First level demonstration of future potential flight experiment
  Utilizes electrolyzer system for hydrogen recycle
Reduction: Automated Unit Design
Simple process diagram illustrating basic system design and electrolyzer integration

## Slide 14
Reduction: Automated Unit Build and Demo
Video speed is 4X actual speed.

## Slide 15
Reduction: Automated System Controls
MMOST Reduction Module Control Schematic, Command Window, and Electronics

## Slide 16
Induction Furnace Heating Rate
Induction Furnace Experiment
Melt Refining: Induction

## Slide 17
Process Options and Evolution
Simple melt coalescence
  Slow
  Small temperature window (iron melt vs. slag sintering)
Slag melting point lowering
  Ca/Si addition (terrestrial process)
  Exact amount and source of raw materials TBD
  Iron recovery from reduced material demonstrated close to 100%
Slag Melting Point Lowering via Ca/Si Addition
Melt Refining: Iron Separation From Slag
Brute Force Melting to Coalesce and Separate Iron from Slgg

## Slide 18
Mold System Past and Current Issues
Heat input limitations – solved
Thermal loss with small sample sizes
Air entrapment
Vertical thermal uniformity
Vertical non-uniformity observed in thermal heating of crucible system
Heating profile of power boosted mold induction system
grooved mold
Melt Refining: Rod Production
current mold system
Iron rod and non-melted granules

## Slide 19
Melt Refining: Vacuum Testing and Automation
Preliminary Automated Melt Unit Designed to Fit in Pioneer Vacuum Chamber

## Slide 20
Induction Melted Iron Grain Texture
Induction Melted Iron Inclusions
Electric Arc Melted Iron Porosity
(edge and center regions)
Melt Refining Materials Characterization
Images courtesy of Peter Corwyn and
Colorado School of Mines

## Slide 21
Wire-fed arc deposition of metallic iron
Colorado School of Mines: Additive Manufacturing
Wheel additively manufactured from commercial analog alloy similar to the MMOST material

## Slide 22
Forward Plans:
Continue operation and refinement of each MMOST process module
Demonstrate units in air and vacuum
  Varying stages of completion already to this point
Integrate unit operations using protocols that minimize peak power demand
Establish mass, volume, power estimates for a scaled-up system
Define path toward mission infusion
Moon to Mars Oxygen and Steel Technology

## Slide 23
Potential Follow-on Activities/Mission Infusion:
LOXIE lunar flight experiment
  Robotic sub-scale system
  Delivered to the Moon on a CLPS lander
Pilot unit operation
  Crewed Artemis mission
  Demonstrate operations and manufacturing in the lunar environment
MMOST commercial system
  Support lunar base operations
  Develop a cis-lunar economy
Moon to Mars Oxygen and Steel Technology

## Slide 24
Acknowledgements:
All project teams and members from Pioneer Astronautics, Colorado School of Mines, and Honeybee Robotics
NASA Johnson Space Flight Center
  Aaron Paz, COR
NASA SBIR program
Moon to Mars Oxygen and Steel Technology

## Slide 25: Backup Slides

## Slide 26
Flow Sheet Development
Lunar Mare – High Ilmenite Case:
For regolith containing ilmenite (FeO·TiO2)
  Suitable for lunar mare regions such as Apollo 11
  Beneficiation via particle size separation, magnetic separation (to remove agglutinates), and electrostatic separation (to boost ilmenite concentration)
Lunar Mare – High FeO Case:
For regolith containing naturally high FeO content
  Suitable for select lunar mare regions, particularly near the South Pole (Artemis)
  Upgrades FeO concentration via particle size separation, magnetic separation (to remove agglutinates), and additional magnetic separation (to boost contained FeO concentration)
Moon to Mars Oxygen and Steel Technology

## Slide 27
Flow Sheet Development
MMOST Primary Process Energy and Power Requirements:
For 35 kg/day iron production rate (10 kg/day oxygen)
Six 4-hour batches per day of feed to iron oxide reduction
20.2 kg beneficiated regolith/batch at 70% ilmenite
Values are for 100% efficiency
Process sequencing and process duration can be adjusted to minimize peak power demand
Heat recovery will be employed when possible
Moon to Mars Oxygen and Steel Technology