## Slide 1: Lunar Physical Simulant Evolution, Production and Use
Jim Richard1, Dale S. Boucher2 and M. M. Battler3 1Electric Vehicle Controllers Ltd. (EVC), 2200 Valleyview Road, Val Caron, Ontario, CANADA P3N 1L1 e-mail jrichard@norcat.org. 2Northern Centre for Advanced Technology Inc. (NORCAT), 1400 Barrydowne Road, Sudbury, Ontario, CANADA P3A 3V8 e-mail dboucher@norcat.org. 3Planetary and Space Science Centre, Department of Geology, University of New Brunswick, Fredericton, NB, E3B 5A3, Canada, melissa.battler@unb.ca,

## Slide 2
Create a test environment for mining techniques and technologies in preparation for planetary surface missions.
Rationale
Regolith Simulant Manufacture and Use
Temperature Environment
Pressure Environment

## Slide 3: NORCAT/EVC - Joint Venture Partners Planetary Mining Equipment Development Since 2000 Core Sampling and Excavation Equipment
E.V.C/NORCAT Joint Venture Partners
Planetary Mining Equipment Development
Since 2000
Core Sampling and Excavation Equipment
Physical simulant is required for relevant testing.
Sufficient quantities of existing simulants were not readily available.
Notes: Hydrogeology drill used as a test unit for all electric core drilling under both Nasa Resolve and CSA sponsored contracts. Frozen ground testing was performed in the field last February.
Test set up that allowed for drilling to depths of up to two meters. This test stand was used last spring for preliminary drill testing using our OB-1 Simulant
Need for a physical lunar simulant was identified early on in our development of lunar drilling equipment under the RESOLVE project. No such simulant was readily available so we began the development of our simulant.

## Slide 4: Directed Research with University of New Brunswick.
Emphasis placed on highland simulant development
Notes: EVC/NORCAT employed the University of New Brunswick- Department of Geology, Planetary and Space Science Centre Under Dr. John Spray and Masters graduate student Melissa Battler to assist us in understanding what we needed to produce an appropriate simulant.
Under RESOLVE our target area is the Permanently shadowed South pole region of the moon and expectations were we would encounter predominantly Highland anorthositic regolith.
We investigated several terrestrial sources of anorthosite in an effort to determine what available material was most appropriate.
This included acquiring actual samples of the following anorthosites. Nain, St.Charles, Shakespeare- Dunlop and the Shawmere. In addition literature studies were completed on other available materials including Stillwater.
A selection was then made.
And now for the first time ever, right here at the Space Resources Roundtable the material selected will be revealed.
And the winner is- Next slide please
The targets ranges of our simulant are based largely on data from Houck (1982), and Morris et al. (1983), for Apollo 16 samples 64501 and 64500, as well as some assumptions for the 500-1000 μm, and 0-20 μm size ranges.

## Slide 5: Shawmere Anorthosite
Material acquired from Avalon Ventures Ltd. Quarry located in Foleyet, Ontario
Custom processing protocol developed using Jaw, Roll and Ring crushers
Particle size testing performed and compared to Apollo 16 Highland Lunar Samples 64501 and 64500
Olivine slag added to enhance abrasive qualities. Combined mix is OB-1
800 kg currently in Production. 15 tons of Anorthosite and 20 tons of Olivine slag stockpiled at EVC
Notes: Material acquired from Avalon Ventures Ltd.. Avalon Ventures Ltd. is a Canadian junior mineral exploration and development company with a primary focus on industrial minerals and rare metals with high technology applications.
Crushing process is a three stage process utilizing a Jaw, Roll and Ring Crusher. The jaw is utilized as a primary crusher for all of the material. The simulant course component is separated out and saved to be mixed later with medium and fine material. The medium and fine components are run through the roll crusher and the medium component is separated out to be mixed later. The fine component is then run through the ring crusher. All three components are then mixed using a Jones riffle.
We performed chemical and mechanical testing and analysis of Shawmere Anorthosite; We analyzed mineralogy as well as grain size and shape distribution, post processing;
One major component missing from the simulant was the glass particles. This component is critical to any physical simulant due to the angularity of the particles which contribute greatly to the abrasive nature and compactability, Both of these properties will have an impact on hardware developed to drill or excavate.
We sourced an Olivine glass slag that was crushed and added to the anorthosite. The mixed simulant is known as ob-1
We are currently have in production 400 kg of OB-1 in production in 10 kg lots.
Mineralogy and Silica content testing as well as particle size distribution information is being gathered for the anorthosite, glass and OB-1 for the purpose of creating Material Safety Data Sheets
We currently have 15 tons of anorthosite and 20 tons of the olive slag stockpiled.

## Slide 6
Cryocooler Chamber
Liquid Nitrogen temperatures
Custom design for in chamber drilling
Compaction
Standardized Proctor & Modified Proctor tests
Custom designed for OB-1 simulant
Range of moistures contents
Cryo capable compaction vessels
Vacuum
The process of obtaining a vacuum may affect the compaction
Specialized techniques required
TEST ENVIRONMENT

## Slide 7
Battler, M.M., Richard, J., Boucher, D., Spray, J.G.,
Progress Report : Development Production of the Lunar Highland Regolith Simulant
Presentation delivered at the PTMSS 2006
References