## Slide 1: Kinetic Investigation of Water-Production from Lunar Soil Simulant by H2 Reduction
Space Resources Roundtable VIII
Nov.1, 2006, Golden, CO
T. Watanabe, S. Komatsuzaki
Tokyo Institute of Technology, Japan
H. Kanamori, S. Aoki
Shimizu Corporation, Japan
Tokyo Tech

## Slide 2: Introduction
Equilibrium
Process selection
Reaction temperature
Yield of products
Recycling efficiency
Kinetics
Heat transfer rate
Electrical power
Reaction rate
Plant design
Site condition
Plant scale
Dependence on terrestrial material
Background
Future missions for lunar exploration and development
  Large scale lunar orbiting mission is planed. (SELENE)
  Lunar resource utilization technologies will be much more important.
Utilization of lunar environment and resource.
  Manned lunar missions require the use of locally derived materials.
Purpose of this study
Selection of appropriate feedstock and process for O2 production
Investigation of reaction mechanism of water-production from lunar soil
Tokyo Tech

## Slide 3: O2 production process
Lunar Regolith
Place | Mineral | Composition
Mare | Ilmenite | FeTiO3
 | Pyroxene | (Fe,Mg)SiO3
 | Olivine | (Fe,Mg)2SiO4
 | Anorthite | CaAl2Si2O8
Highland | Anorthite | CaAl2Si2O8
Possible Reducing Agents
H2, CO，CH4, C, F2
Water-production is a primary concern for lunar resources utilization.
Selection of adequate feedstock and reducing agents for lunar resources processing
O2 Production
Tokyo Tech
Water and O2 are essential for manned lunar mission.

## Slide 4: Thermodynamic consideration
Iron-bearing minerals can be easily reduced by H2.
Anorthite can be reduced only by F2.
Mare
Highland
Ilmenite (FeTiO3)
Anorthite (CaAl2Si2O8)
Tokyo Tech

## Slide 5: O2 production Process
Fe + TiO2
CO Reduction of FeTiO3 (1200 K)
H2 Reduction of CO2 (1100 K)
Electrolysis
(373 K)
CO2
CO
H2O
H2
O2
FeTiO3
+226 kJ
-196 kJ
-11.2 kJ
+6.78 kJ
-137 kJ
+43.2 kJ
CO reduction of ilmenite
H2
Electrolysis
(373 K)
H2 Reduction of FeTiO3 (1200 K)
H2O
Fe + TiO2
FeTiO3
+226 kJ
-196 kJ
-146 kJ
+54.0 kJ
H2 reduction of ilmenite
Required energy of preheating or cooling
O2
Production for 1-mol O2
Tokyo Tech
Understanding of the H2 reduction mechanism of ilmenite is important for the mission
of lunar soil utilization.

## Slide 6: Experiments of H2 reduction
Component | Lunar Soil Apollo14 [ wt% ] | Lunar Soil Simulant [ wt% ]
SiO2 | 48.1 | 50.3
Al2O3 | 17.4 | 16.3
CaO | 10.7 | 9.4
MgO | 9.4 | 4.4
FeO | 10.4 | 8.7
Fe2O3 | - | 4.4
Others | 3.8 | 6.5
Total | 99.8 | 100.0
Water-production from lunar soil simulant by H2 reduction
Investigation of the kinetics and the mechanism
using thermogravimetry and fixed bed reactor.
Chemical composition of lunar soil simulant
Lunar soil simulant was made by Shimizu Co., Japan.
Median diameter: 70 m.
Simulant has almost the same composition with lunar soil.
Fe2O3 is included in simulant.
Tokyo Tech

## Slide 7: Fixed bed reactor
H2 Flow Rate
Sample Weight
Reaction Temperature
Particle Size
Inlet Pressure
[ L/min ]
[ g ]
[ K ]
[ m ]
[ kPa ]
4, (2, 6)
10, (3, 5, 15)
1073, 1173, 1223, 1273, 1323
70, (30, 120)
303
Experimental Conditions
H2
He
Heated line
Temperature
H2 flow line
Pressure
Moisture meter
Back pressure valve
Sample
H2 flow line
Inlet temperature
Sample temperature
Heater
Tokyo Tech

## Slide 8: Fixed bed reactor
Sample
Gas inlet
Gas outlet
100 mm
Thermocouple
Outer tube
Gas inlet
Inner tube
Thermocouple
Gas outlet
Sample
Fin
Filter
Tokyo Tech

## Slide 9: SEM observation
Before reduction
After reduction
at 1288 K
After reduction
at 1338 K
As reduction proceeds…
White parts (ilmenite) have several holes.
The pores were blocked by the melt of alkali contents at 1338 K.
Tokyo Tech
 | before | 5 min
SiO2 | 50.90 | 51.30
Al2O3 | 16.00 | 16.22
TiO2 | 2.11 | 2.19
Fe | 0.11 | 3.47
Fe2O3 | 4.25 | 0.07
FeO | 8.47 | 7.95
Soil Contents [ wt% ]

## Slide 10: Effect of temperature
Water-production rate increases with temperature up to 1273 K.
Decrease in water-production rate over 1273 K is due to melted part of glassy contents.
Tokyo Tech

## Slide 11: Thermogravimetry
Experimental Conditions
Sample
Gas Inlet
Gas Outlet
Furnace
Thermocouple
Thermobalance
Temperature [ K ] 973, 1023, 1073, 1123, 1173, 1223, 1273
H2 Concentration [ mol/L ] 8.93×10-4, 1.34×10-3, 1.79×10-3
Sample Weight [ mg ] 100
Particle Size [ m ] 70, (30, 120)
Tokyo Tech

## Slide 12: Result of H2 reduction (TG)
Sample: 100 mg
3%-H2 injection
at 1173 K
R : Reaction rate [ mol kg-1 s-1 ]
k : Rate constant [ L kg-1 s-1 ]
CH2 : H2 conc. [ mol L-1 ]
E : Activation energy [J mol-1]
Rate equation
Order of reaction
Rate constant
Activation energy
Rate-controlling step
Arrhenius equation
Tokyo Tech

## Slide 13: Effect of H2 concentration
Reduction is 1st-order reaction with H2 concentration.
High-concentration of H2
High reaction rate
Tokyo Tech

## Slide 14: Arrhenius plot
Fractional Weight Loss [ - ] | Activation Energy [ kJ/mol ]
0.001 | 50.2
0.004 | 77.4
0.009 | 82.3
Fe2O3 + H2 → 2FeO + H2O
FeO + H2 → Fe + H2O
Tokyo Tech

## Slide 15: Conclusions
The reduction is first-order reaction with H2 concentration.
Initial stage is reduction of Fe2O3.
FeTiO3 and FeO are reduced at the following stage.
Reaction rate of FeO reduction should be estimated.
H2 reduction is optimum process for O2 production from ilmenite on the moon.
Chemical reaction is rate-controlling step.
Fixed bed reactor
Reaction mechanism
Tokyo Tech

## Slide 16: Comparison of process
Reduction Agent | Recycle Method | Approved Technology | Number of Step | Highest Temperature [ K ] | Required Energy [ kJ ] | Exothermic Heat [ kJ ] | Feedstock | Product Value | Rank
H2 | Electrolysis of H2O | ○ | 2 | 1200 | 762 | 147 | mare | ○ | 1
CO | H2 reduction of H2O | ○ | 3 | 1200 | 737 | 157 | mare | ○ | 2
CO | Electrolysis of CO2 | × | 2 | 1200 | 778 | 200 | mare | ○ | 5
CO | Pyrolysis of CO2 | × | 2 | 3344 | 774 | 196 | mare | × | 6
CH4 | Methanation | ○ | 3 | 1000 | 1178 | 600 | mare | × | 4
CH4 | Sabatier reaction | ○ | 3 | 1288 | 914 | 342 | mare | ○ | 3
F2 | H reduction of fluoride | × | 4 | 3748 | 2340 | 1060 | highland and mare | × | 7
H2 reduction is optimum process.
Tokyo Tech

## Slide 17: Equilibrium composition
Equilibrium composition of FeTiO3-H2 system
FeTiO3 : H2 = 1 : 1
Tokyo Tech

## Slide 18: Result of H2 reduction
Initial reduction rate is rapid, followed by rapid decrease.
Experimental Conditions
Simulant: 10 g, H2: 4 L/min, 1173 K, 303 kPa
Tokyo Tech

## Slide 19: Effect of particle size
Insufficient reduction at inner part of larger particles
Smaller particle
Higher rate of weight loss
Larger weight loss
Tokyo Tech

## Slide 20: XRD analysis
Before reduction
After reduction
Tokyo Tech

## Slide 21: Effect of H2 flow rate
Smaller hydrogen flow rate Lower water production rate
Higher H2O concentration in gas phase depresses the reaction.
Tokyo Tech

## Slide 22: Effect of sample weight
Water-production rate per unit weight is equal in the case of 5 g and 3 g.
Tokyo Tech

## Slide 23: Estimation of resistance
Shrinking core model
Chemical reaction is rate-controlling step.
Ash
Gas Film
Unreacted core
X
0
rc
Rp
Gas film diffusion
Intraparticle diffusion
Chemical reaction
Tokyo Tech