## Slide 1: Modeling of Agglutinates and its mechanical properties
Tryana Garza-Cruz
Masami Nakagawa
Colorado School of Mines

## Slide 2: Regolith Modeling
Efficient and safe processing of Lunar Soil is necessary for a sustainable stay on the Moon. The ability to predict and understand the mechanical properties of lunar soil will ensure the development of novel machinery to extract and process the regolith.
We have developed a set of simulations to model the behavior and properties of lunar soil found in laboratory experiments and the ways they may break into finer particles.

## Slide 3: Particle Flow Code 2D
PFC2D is a 2D discontinuum program based on Distinct Element Method (DEM). This method was introduced for the analysis of rock-mechanics problems and enables us to have two bonding models; Contact-bond and Parallel-bond.
The parallel-bond is like a finite-sized piece of cementation deposited between particles. It can be used to simulate the mechanical behavior of different materials and therefore the way they break into finer particles.
How do they break?
Parallel bond

## Slide 4: DEM Representation
In DEM a rock can be represented as a dense packing of particles bonded together at their contact points

## Slide 5: Fracture of simple geometries
Notes: prop dens 2500 kn 1e8 ks 1e8 fric 0.2
property pb_rad 1 pb_s 1e6 pb_n 1e6
property pb_kn 2e6 pb_ks 2e6
wall id 1 kn=1e8 ks=1e8 fric 0.5
ball rad 0.5
Six balls
ball rad 0.5
wall id 1 kn=1e8 ks=1e8 fric 0.5
prop dens 2500 kn 1e8 ks 1e8 fric 0.2
set grav 0 -9.81
property pb_rad 1 pb_s 1e6 pb_n 1e6
property pb_kn 3e6 pb_ks 3e6

## Slide 6: Virtual Agglutinates

## Slide 7: Uniaxial Compression test of one Virtual Agglutinate
Notes: pro den 3000 kn 1e8 ks 1e8
pro fric 1
set gra 0 -9.81
pro pb_rad 1 pb_kn 1e9 pb_ks 1e9 pb_nstr 1e4 pb_sstr 1e4

## Slide 8: One dimensional Oedometer test
Apollo 12 Carrier et al.(1972b,1973c)
Luna 16 and 20 Leonovich et al. (1974a,1975)

## Slide 9: Compressibility
Compressibility describes the volume change, or densification, that occurs when a confining stress is applied to soil.
At low stresses compression of the soil results from particle slippage and reorientation.
At high stress, particle deformation and breakage at the points of contact also occur.
Void ratio n : porosity
Compressibility:
σv : applied vertical stress

## Slide 10: Three Different Models

## Slide 11: Uniaxial Compression Test of a bed of agglutinates

## Slide 12: Simulation results

## Slide 13: Uniaxial Compression Test of a bed of agglutinates and uniform size particles

## Slide 14: Agglutinates and particles

## Slide 15: Uniaxial Compression Test of a bed of agglutinates and particles with size distribution

## Slide 17: One dimensional Oedometer test
Apollo 12 Carrier et al.(1972b,1973c)
Luna 16 and 20 Leonovich et al. (1974a,1975)

## Slide 18: THANK YOU
Questions?